Copyright 2024 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to The Pittsburgh Paints Company (formerly PPG Paints) ("Licensee"). The Pittsburgh Paints Company is the exclusive distributor of PPG Protective and Marine Coatings products.

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact The Pittsburgh Paints Company, 400 Bertha Lamme Dr., Cranberry Township, PA 16066; Phone: (888) PPG-IDEA | (888) 774-4332, Option 4; Website: www.pittsburghpaints.com; Email: ppgspec@ppg.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 099124 - INTERIOR PAINTING (MPI STANDARDS)

Access Manufacturer's Specpoint Product Cards:

<Double click here to view the manufacturer's product cards available at Deltek Specpoint>

GENERAL

SUMMARY

Section Includes: Surface preparation of substrates and application of the following:

Interior paint systems.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed products and insert references to this Section to establish primer requirements.

[Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming structural steel substrates.

Section 055000 "Metal Fabrications" for shop priming metal fabrications.

Section 055113 "Metal Pan Stairs" for shop priming metal pan stairs.

Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

[Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

Section 099114 "Exterior Painting (MPI Standards)."

Section 099301 "Staining and Transparent Finishing (MPI Standards)" for surface preparation and the application of wood stains and transparent finishes on interior wood substrates.

Section 099601 "High-Performance Coatings (MPI Standards)" for tile-like coatings.

DEFINITIONS

Definitions of MPI Gloss Levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

MPI Gloss Level G1: Not more than 5 units at 60 degrees and 10 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G2: Not more than 10 units at 60 degrees and between 10 to 35 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G3: Between 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G4: Between 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G5: Between 35 to 70 units at 60 degrees, in accordance with ASTM D523.

MPI Gloss Level G6: Between 70 to 85 units at 60 degrees, in accordance with ASTM D523.

MPI Gloss Level G7: More than 85 units at 60 degrees, in accordance with ASTM D523.

ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

Product Data: For each type of product.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

Include preparation requirements and application instructions.

Indicate VOC content.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples. Delete "Samples" and "Samples for Initial Selection" paragraphs if colors and other characteristics are preselected and specified or scheduled and only verification Samples are required.

Samples: For each type of topcoat product.

Samples for Initial Selection: For each type of topcoat product.

Samples for Verification: For each type of paint system and in each color and gloss of topcoat. Submit [actual paint drawdowns as specified below] [paint manufacturer's standard printed cards] for verification Samples.

Retain subparagraphs below only if retaining option above for actual paint drawdowns for verification Samples. Color and gloss of Samples change as they age; seven-day old Samples appear different from freshly dried Samples.

Submit Samples on rigid backing, 8 inches (200 mm) square.

Apply coats on Samples in steps to show each coat required for system.

Label each coat of each Sample.

Label each Sample for location and application area.

Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in the Interior Painting Schedule to cross-reference paint systems specified in this Section. Include color designations.

Retain "Sustainable Design Submittals" Paragraph below if required to attain sustainability rating or to track sustainability submittals.

Sustainable Design Submittals:

"Product Data" Subparagraph below applies to LEED v4, LEED v4.1, IgCC/ASHRAE 189.1, Green Globes, and CALGreen. Coordinate with requirements for paints and coatings.

Product Data: For paints and coatings, indicating VOC content.

"Environmental Product Declaration (EPD)" Subparagraph below applies to LEED v4 (all) MR Credit "Building Product Disclosure and Optimization - Environmental Product Declarations." Verify, with manufacturer, that EPDs are available for each product.

Environmental Product Declaration (EPD): For each product.

"Health Product Declaration (HPD)" Subparagraph below applies to LEED v4 (all) MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting." Verify, with manufacturer, that HPDs are available and comply with requirements of the HPD Open Standard or USGBC-approved program.

Health Product Declaration (HPD): For each product.

"Sourcing of Raw Materials" Subparagraph below applies to LEED v4 (all) MR Credit "Building Project Disclosure and Optimization - Sourcing of Raw Materials," Option 1 - "Raw Material Source and Extraction Reporting." Verify, with manufacturer, that corporate sustainability reports are available, have been prepared within the last year or are applicable to the year of production, and are by USGBC-approved organization.

Sourcing of Raw Materials: Corporate sustainability report for each manufacturer.

"Environmental Product Declaration (EPD)" Subparagraph below applies to LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Environmental Product Declarations." Verify, with manufacturer, that EPDs are available for each product. Use at least 20 different permanently installed products from at least five different manufacturers.

Environmental Product Declaration (EPD): For each product.

"Health Product Declaration (HPD)" Subparagraph below applies to LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting." Verify, with manufacturer, that HPDs are available and comply with requirements of the HPD Open Standard or USGBC-approved program.

Health Product Declaration (HPD): For each product.

"Sourcing of Raw Materials" Subparagraph below applies to LEED v4.1 (all) MR Credit "Building Project Disclosure and Optimization - Sourcing of Raw Materials," Option 1 - "Raw Material Source and Extraction Reporting." Verify, with manufacturer, that corporate sustainability reports are available, have been prepared within the last year or are applicable to the year of production, and are by USGBC-approved organization.

Sourcing of Raw Materials: Corporate sustainability report for each manufacturer.

Retain first "Environmental Product Declaration (EPD)" Subparagraph below if products specified in this Section are required to have an EPD to comply with IgCC/ASHRAE 189.1's requirement of 55 percent recycled materials.

Environmental Product Declaration (EPD): For each product.

First "Environmental Product Declaration (EPD)" Subparagraph below applies to IgCC/ASHRAE 189.1 if products specified in this Section are used to comply with requirements of paragraph 9.4.1.4, "Multiple-Attribute Product Declaration or Certification," which require EPDs for a minimum of 10 products.

Environmental Product Declaration (EPD): For each product.

Three subparagraphs below apply to Green Globes v1.4 if products specified in this Section are used to comply with requirements of paragraph 3.5.1.2, "Path B: Prescriptive Path for Building Core and Shell," which require that a certain percentage of materials used in the core and shell have EPDs, third-party certifications, and/or third-party life-cycle assessments.

Environmental Product Declaration (EPD): For each product.

Third-Party Certifications: For each product.

Third-Party-Certified Life-Cycle Assessment: For each product.

MAINTENANCE MATERIAL SUBMITTALS

See Section 017700 "Closeout Procedures" for submission of maintenance material items.

Furnish extra materials that match paint products applied and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint Products" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

Paint Products: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert number> of each material and color applied.

MOCKUPS

Apply mockups of each paint system indicated and each color and finish selected to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

Architect will select one surface to represent surfaces and conditions for application of each paint system.

Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

Other Items: Architect will designate items or areas required.

Final approval of color selections will be based on mockups.

If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Owner specifically approves such deviations by Change Order.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

Maintain containers in clean condition, free of foreign materials and residue.

Remove rags and waste from storage areas daily.

FIELD CONDITIONS

Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

Do not apply paints when relative humidity exceeds 85 percent; at temperatures of less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Retain "Source Limitations" Article below to limit sources for the entire Section. Source limitations may also be specified in individual articles if desired.

SOURCE LIMITATIONS

Obtain each paint product from single source from single manufacturer.

INTERIOR PAINTS, GENERAL

Retain "Interior Paint Systems" Paragraph below and include list of manufacturers if desired, in addition to MPI standards indicated and listed below.

See lists of products currently approved by MPI in its "MPI Approved Products List." See the "Writing Guide" Article in the Evaluations for further discussion.

Interior Paint Systems: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include but are not limited to products] listed in the applicable interior painting schedule articles for the paint category indicated.

Retain "Basis-of-Design Product" Paragraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; products as designated in the Interior Painting Schedule for the paint category indicated or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

MPI Standards: Provide products complying with MPI standards indicated in applicable interior painting schedule articles and listed in the "MPI Approved Products List."

Generally, retain "Material Compatibility" Paragraph below. Systems could fail if paints used for separate coats are incompatible. MPI's paint systems match primers and topcoats and take compatibility into consideration.

Material Compatibility:

Materials for use within each paint system to be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

For each coat in a paint system, products must be recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

"VOC Content" and "Low-Emitting Materials" paragraphs below apply to LEED v4 and LEED v4.1 EQ Credit "Low-Emitting Materials." Delete option in "VOC Content" Paragraph for LEED v4.1 for Schools and LEED v4.1 for Healthcare credit for exterior-applied products.

For interior applications, LEED v4.1 compliance, 100 percent of interior applied paint and coatings products by volume must comply with wet-applied VOC-content limits. Paint and coatings wet-applied on-site must comply with applicable VOC limits of the California Air Resources Board (CARB) 2007, Suggested Control Measure (SCM) for Architectural Coatings, or the South Coast Air Quality Management District (SCAQMD) Rule 1113, effective February 5, 2016. Both CARB 2007 SCM and SCAQMD Rule 1113 are cited in LEED v4.1, EQc 2, "Low-Emitting Materials Reference Guide." Choose one wet-applied VOC-content-limit compliance path below, either CARB or SCAQMD.

For CARB 2007 SCM, see https://ww2.arb.ca.gov/our-work/programs/coatings/architectural-coatings/suggested-control-measure.

For SCAQMD Rule 1113 (more restrictive), see latest updated version amended February 5, 2016 at www.aqmd.gov/docs/default-source/rule-book/reg-xi/r1113.pdf.

VOC Content: For field applications[ that are inside the weatherproofing system], verify paints and coatings comply with VOC content limits of authorities having jurisdiction and the following VOC content limits:

Categories in subparagraphs below are taken from LEED rating systems and the standards referenced by them; if clarification is required, see those documents or the reference guides.

In general, avoid MPI systems using alkyd primers and topcoats for compliance with LEED v4.1. These products are not likely to comply with VOC content cutoff limits or the emissions certification requirements of LEED v4.1.

SCAQMD and CARB apply to "Flat Paints and Coatings" Subparagraph below.

Flat Paints and Coatings: 50 g/L.

Retain first option in "Nonflat Paints and Coatings" Subparagraph below for SCAQMD; second, for CARB.

Nonflat Paints and Coatings: [50] [150] g/L.

Retain first option in "Nonflat Paints and Coatings (High Gloss)" Subparagraph below for SCAQMD; second, for CARB.

Nonflat Paints and Coatings (High Gloss): [50] [150] g/L.

Dry-Fog Coatings: 150 g/L.

Primers, Sealers, and Undercoaters: 100 g/L.

Retain first option in "Rust-Preventive Coatings" below for South Coast; second, for CARB.

Rust-Preventive Coatings: [100] [250] g/L.

Retain first option in "Zinc-Rich Industrial Maintenance Primers" Subparagraph below for SCAQMD; second, for CARB.

Zinc-Rich Industrial Maintenance Primers: [100] [340] g/L.

Pretreatment Wash Primers: 420 g/L.

Floor Coatings: [50] [100] g/L.

Shellacs, Clear: 730 g/L.

Shellacs, Pigmented: 550 g/L.

Low-Emitting Materials: For field applications that are inside the weatherproofing system, verify 90 percent of paints and coatings comply with requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

"Material Emissions and Pollutant Control" Paragraph below applies to IgCC/ASHRAE 189.1.

Material Emissions and Pollutant Control: Verify not less than 85 percent of field-applied paints and coatings that are inside the weatherproofing system comply with either of the following:

Low-Emitting Materials: Verify VOC emissions comply with requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." Verify formaldehyde emissions do not exceed 9 mcg/cu. m or 7 ppb, whichever is less.

Verify VOC content does not exceed limits of authorities having jurisdiction and the following:

Flat Coatings: 50 g/L.

Nonflat Coatings: 100 g/L.

Nonflat - High-Gloss Coatings: 150 g/L.

Concrete/Masonry Sealers: 100 g/L.

Floor Coatings: 100 g/L.

Industrial Maintenance Coatings: 250 g/L.

Low-Solids Coatings: 120 g/L.

Mastic Texture Coatings: 100 g/L.

Metallic Pigmented Coatings: 500 g/L.

Pretreatment Wash Primers: 420 g/L.

Primers, Sealers, and Undercoaters: 100 g/L.

Reactive Penetrating Sealers: 350 g/L.

Recycled Coatings: 250 g/L.

Rust-Preventive Coatings: 250 g/L.

"VOC Emissions" Paragraph below applies to Green Globes.

VOC Emissions: For field applications inside the building, wall paints to contain no more than half of the chronic REL of VOCs when tested in accordance with the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." The building concentration of formaldehyde will not exceed half of the indoor recommended exposure limit or 33 mcg/cu. m and that of acetaldehyde will not exceed 9 mcg/cu. m.

Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule on Drawings] <Insert requirements>.

[10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in subparagraphs below are based on MPI recommendations.

Concrete: 12 percent.

Cementitious Composition Board: 12 percent.

Masonry (Clay and CMUs): 12 percent.

Wood: 15 percent.

Gypsum Board: 12 percent. Verify that finishing compound is dry and sanded smooth.

Plaster: 12 percent. Verify that plaster is fully cured.

Verify suitability of substrates, including surface conditions and compatibility, with finishes and primers. Proceed with coating application only after unsatisfactory conditions have been corrected.

Application of coating indicates acceptance of surfaces and conditions.

PREPARATION

For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in the Interior Painting Schedule.

Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates and paint systems indicated.

Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

Steel Substrates: Remove loose rust, loose mill scale, loose shop primer, and other loose foreign matter. Clean using methods recommended in writing by paint manufacturer[.] [ but not less than the following:]

Usually, retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

SSPC-SP 2.

SSPC-SP 3.

SSPC-SP 7/NACE No. 4 "Brush-Off Blast Cleaning" permits tight residues of rust, mill scale, and coatings to remain. "Commercial Blast Cleaning" methods specified in SSPC-SP 6/NACE No. 3 may be impractical for use at Project site or allowed by authorities having jurisdiction.

SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized Metal Substrates: Remove grease and oil residue from galvanized metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

Aluminum Substrates: Remove loose surface oxidation.

Wood Substrates:

Scrape and clean knots. Before applying primer, apply coat of knot sealer recommended in writing by topcoat manufacturer for interior use in paint system indicated.

Sand surfaces that will be exposed to view and remove sanding dust.

Prime edges, ends, faces, undersides, and backsides of wood.

After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

Canvas and Cotton Insulation Covering Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

Plastic Trim Fabrication Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

APPLICATION OF INTERIOR PAINT PRODUCTS

Apply paints in accordance with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual."

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

Use applicators and techniques suited for paint and substrate indicated.

Paint surfaces behind movable equipment and furniture same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed equipment or furniture with prime coat only.

Paint front and backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

Retain first subparagraph below if required for steel windows.

Paint entire exposed surface of window frames and sashes.

Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

Primers specified in applicable interior painting schedule articles may be omitted on items that are factory primed or factory finished if compatible with intermediate and topcoat coatings and acceptable to intermediate and topcoat paint manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Tint undercoats to match color of topcoat but provide sufficient difference in shade of undercoats to distinguish each separate coat.

If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

Painting Fire-Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

First subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

Paint the following work where exposed to view in equipment rooms:

Subparagraphs below contain items that are often field painted, plus others that are often not. Revise list to suit Project.

Equipment, including panelboards[ and switch gear].

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Tanks that do not have factory-applied final finishes.

Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

<Insert mechanical items to be painted>.

Paint the following work where exposed to view in occupied spaces:

Subparagraphs below contain items that are usually field painted, plus others that are often not. Revise list to suit Project.

Equipment, including panelboards.

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

Other items as directed by Architect.

<Insert mechanical items to be painted>.

Paint portions of internal surfaces of metal ducts, without liner, behind air inlets and outlets that are visible from occupied spaces.

FIELD QUALITY CONTROL

Dry Film Thickness Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for dry film thickness.

Touch up and restore painted surfaces damaged by testing.

If test results show that dry film thickness of applied paint does not comply with paint manufacturer's written recommendations, apply additional coats as needed to provide dry film thickness that complies with paint manufacturer's written recommendations.

Cost of retesting is Contractor's responsibility.

CLEANING AND PROTECTION

At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

Do not clean equipment with free-draining water and prevent solvents, thinners, cleaners, and other contaminants from entering into waterways, sanitary and storm drain systems, and ground.

Dispose of contaminants in accordance with requirements of authorities having jurisdiction.

Allow empty paint cans to dry before disposal.

Retain subparagraph below if paint recycling or collection facilities are available in vicinity of Project.

Collect waste paint by type and deliver to recycling or collection facility.

After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

INTERIOR PAINTING SCHEDULE, CONCRETE SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Vertical (Nontraffic) Surfaces:

Latex System: MPI INT 3.1A.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Zero Interior Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Latex Aggregate System: MPI INT 3.1B.

Prime Coat: Textured coating, latex, flat, MPI #42.

Pittsburgh Paints' "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Zero Interior Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex Aggregate System: MPI INT 3.1N.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Pittsburgh Paints' "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Topcoat: Textured latex coating, flat, MPI #42.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 3.1M.

Prime Coat: Primer sealer, interior, institutional low odor/VOC, MPI #149.

Pittsburgh Paints; Speedhide Zero Interior Latex Sealer, 6-4900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance 100% Acrylic Latex Primer, 9-900 Series; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 3.1C.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 3.1L.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 3.1D.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Concrete Stain System: MPI INT 3.1K.

For a Premium Grade system, "MPI Manual" requires first coat; delete "First Coat" Subparagraph below for a Budget Grade system.

First Coat: Stain, interior, matching topcoat.

Topcoat: Stain, interior, MPI #58.

Pittsburgh Paints' "Perma-Crete Color Seal WB" is LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less.

Pittsburgh Paints; Perma-Crete Color Seal WB Interior/Exterior 100% Acrylic Concrete Stain, 4-4210XI Series; applied at 1.3 mils minimum DFT.

Horizontal (Traffic) Surfaces:

Latex Floor Enamel System: MPI INT 3.2A.

Prime Coat: Floor paint, latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Floor paint, latex, matching topcoat.

Topcoat: Floor paint, latex, low gloss.

Pittsburgh Paints' "Floor & Porch 100% Acrylic Latex Satin, 3-510XI Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less (CARB Floor Coatings).

Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510XI Series; applied at 1.0 mil minimum DFT.

Alkyd Floor Enamel System: MPI INT 3.2B.

Prime Coat: Floor enamel, alkyd, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Floor enamel, alkyd, matching topcoat.

Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level G6).

Pittsburgh Paints; Floor & Porch Waterborne Alkyd Gloss, 3-610 Series; applied at 1.3 mils minimum DFT.

Concrete Stain System: MPI INT 3.2E.

For a Premium Grade system, "MPI Manual" requires first coat; delete "First Coat" Subparagraph below for a Budget Grade system.

First Coat: Stain, interior, for concrete floors, matching topcoat.

Topcoat: Stain, interior, for concrete floors.

Pittsburgh Paints' "Perma-Crete Color Seal WB" is LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less.

Pittsburgh Paints; Perma-Crete Color Seal WB Interior/Exterior 100% Acrylic Concrete Stain, 4-4210XI Series; applied at 1.3 mils minimum DFT.

Water-Based Concrete Floor Sealer System: MPI INT 3.2G.

For a Budget Grade system, "MPI Manual" requires first coat; "MPI Manual" does not include a Premium Grade system.

First Coat: Sealer, water based, for concrete floors, matching topcoat.

Topcoat: Sealer, water based, for concrete floors, MPI #99.

Pittsburgh Paints' "Perma-Crete Plex-Seal WB" is LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less.

Pittsburgh Paints; Perma-Crete Plex-Seal WB Interior/Exterior 100% Acrylic Clear Sealer, 4-6200XI Series; applied at 0.8 mil minimum DFT.

Latex Zone/Traffic-Marking Paint System: MPI INT 3.2H.

Traffic-marking paint, latex, MPI #97.

Pittsburgh Paints; Ennis Flint Federal Specification Fast Dry Waterborne Paint, 98520x Series.

Pittsburgh Paints; Ennis Flint Fast Dry Waterborne Paint, 98530x Series.

Alkyd Zone/Traffic-Marking Paint System: MPI INT 3.2J.

Traffic-marking paint, solvent based, MPI #32.

Pittsburgh Paints; Ennis Flint Low VOC Traffic Paint, 98530x Series.

INTERIOR PAINTING SCHEDULE, CEMENTITIOUS SUBSTRATES

Cementitious Composition Board Substrates: [Siding] [Trim] [Panels] <Insert requirements>.

Latex System: MPI INT 3.3A.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 3.3G.

Prime Coat: Primer sealer, interior, institutional low odor/VOC, MPI #149.

Pittsburgh Paints; Speedhide Zero Interior Latex Sealer, 6-4900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance 100% Acrylic Latex Primer, 9-900 Series; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five options "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 3.3B.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 3.3H.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 3.3C.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and 7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

INTERIOR PAINTING SCHEDULE, MASONRY SUBSTRATES

Clay Masonry Substrates:

Latex System: MPI INT 4.1A.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex Aggregate System: MPI INT 4.1B.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: Primer for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Intermediate Coat: Intermediate coat for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Pittsburgh Paints' "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Topcoat: Textured coating, latex, flat, MPI #42.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 4.1M.

Prime Coat: Primer sealer, interior, institutional low odor/VOC, MPI #149.

Pittsburgh Paints; Speedhide Zero Interior Latex Sealer, 6-4900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance 100% Acrylic Latex Primer, 9-900 Series; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 4.1L.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 4.1C.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 4.1D.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Pittsburgh Paints' "Speedhide Interior/Exterior WB Alkyd" product line, at 100 g/L or less, complies with VOC content limits in accordance with LEED v4.1.

Retain one of four "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3), MPI #51.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

CMU Substrates:

Latex System: MPI INT 4.2A.

Prime Coat: Block filler, latex, interior/exterior, MPI #4.

Pittsburgh Paints' "Speedhide 6-15XI" and "Perma-Crete 4-100XI" block fillers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide 6-15XI."

Pittsburgh Paints: Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex Aggregate System: MPI INT 4.2B.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: Primer for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Intermediate Coat: Intermediate coat for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Pittsburgh Paints' "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Topcoat: Textured coating, latex, flat, MPI #42.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 4.2E.

Block Filler: Block filler, latex, interior/exterior, MPI #4.

Pittsburgh Paints' "Speedhide 6-15XI" and "Perma-Crete 4-100XI" block fillers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide 6-15XI."

Pittsburgh Paints: Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: [MPI INT 4.2D] [MPI INT 4.2P].

Retain "Block Filler" or "Prime Coat" Subparagraph below. First subparagraph corresponds to MPI INT 4.2D; second corresponds to MPI INT 4.2P.

Block Filler: Latex, interior/exterior, MPI #4.

Pittsburgh Paints' "Speedhide 6-15XI" and "Perma-Crete 4-100XI" block fillers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide 6-15XI."

Pittsburgh Paints: Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints' "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series" and "Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI" primers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series."

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 4.2K.

Block Filler: Latex, interior/exterior, MPI #4.

Pittsburgh Paints' "Speedhide 6-15XI" and "Perma-Crete 4-100XI" block fillers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide 6-15XI."

Pittsburgh Paints: Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

For areas subject to wetting, consider using epoxy system MPI INT 4.2G, which is specified in Section 099600 "High-Performance Coatings," instead of alkyd system in "Alkyd System" Subparagraph below.

Alkyd System: [MPI INT 4.2C] [MPI INT 4.2N].

Block Filler: Latex, interior/exterior, MPI #4.

Pittsburgh Paints' "Speedhide 6-15XI" and "Perma-Crete 4-100XI" block fillers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide 6-15XI."

Pittsburgh Paints: Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

Retain "Sealer Coat" Subparagraph below for MPI INT 4.2N; delete for MPI INT 4.2C.

Sealer Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints' "Speedhide 6-2," "Speedhide 6-4900XI," and "Pure Performance 9-900" primers comply with wet-applied VOC-content limits and emission requirements of LEED v4.1.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

INTERIOR PAINTING SCHEDULE, METAL SUBSTRATES

Steel and Iron Substrates:

Latex System, Alkyd Primer: [MPI INT 5.1Q] [MPI INT 5.1QQ].

Retain one of two "Prime Coat" subparagraphs below for field-applied prime coat. First corresponds to MPI INT 5.1Q; second corresponds to MPI INT 5.1QQ.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide LV Rust-Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph only if applicable. If retaining, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Shop-Applied Quick-Drying Shop Primer System: MPI INT 5.1X.

Prime Coat: Primer, quick dry, for shop application, MPI #275.

Pittsburgh Paints: Quick Dry Shop Coat Primer, 4190 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 5.1S.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: [MPI INT 5.1R] [MPI INT 5.1RR].

Retain one of two "Prime Coat" subparagraphs below for field-applied prime coat. First corresponds to MPI INT 5.1R; second corresponds to MPI INT 5.1RR.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide LV Rust-Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph only if applicable. If retaining, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 5.1B.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Water-Based Light Industrial Coating System over Epoxy Primer System: MPI INT 5.1N.

Prime Coat: Primer, epoxy, anticorrosive, MPI #101.

PPG Protective and Marine Coatings; Amerlock 2 AL Aluminum Epoxy Mastic; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amercoat 235 Multi-Purpose Phenalkamine Epoxy; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amerlock 600 High Build Semi-Gloss Epoxy Coating; applied at 5.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Water-Based Dry-Fall System: [MPI INT 5.1C] [MPI INT 5.1CC] [MPI INT 5.1Z].

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Retain one of two "Prime Coat" subparagraphs below for field-applied prime coat. First corresponds to MPI INT 5.1C; second corresponds to MPI INT 5.1CC.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide LV Rust-Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph below only for MPI INT 5.1Z.

Shop-Applied Prime Coat: Primer, quick dry, for shop application, MPI #275.

Pittsburgh Paints: Quick Dry Shop Coat Primer, 4190 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints' "Speedhide Super Tech WB Latex Dry Fog" line is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide Super Tech WB Flat 6-725XI" or "Speedhide Super Tech WB Semi-Gloss 6-727XI."

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Dry fall, latex, flat, MPI #118.

Pittsburgh Paints; Speedhide Super Tech WB Interior Latex Dry Fog, Flat 6-725XI Series; applied at 2.2 mils minimum DFT.

Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level G1).

Pittsburgh Paints; Speedhide Super Tech WB Interior Latex Dry Fog, Flat 6-725XI Series; applied at 2.2 mils minimum DFT.

Topcoat: Dry fall, latex (MPI Gloss Level G3), MPI #155.

Pittsburgh Paints; Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Eggshell 6-724XI Series; applied at 2.0 mils minimum DFT.

Topcoat: Dry fall, water based, for galvanized steel (MPI Gloss Level G3).

Pittsburgh Paints; Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Eggshell 6-724XI Series; applied at 2.0 mils minimum DFT.

Topcoat: Dry fall, latex (MPI Gloss Level G5), MPI #226.

Pittsburgh Paints; Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Semi-Gloss 6-727XI Series; applied at 2.2 mils minimum DFT.

Topcoat: Dry fall, water based, for galvanized steel (MPI Gloss Level G5).

Pittsburgh Paints; Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Semi-Gloss 6-727XI Series; applied at 2.2 mils minimum DFT.

Alkyd System: [MPI INT 5.1E] [MPI INT 5.1EE].

Retain one of two "Prime Coat" subparagraphs below for field-applied prime coat. First corresponds to MPI INT 5.1E; second corresponds to MPI INT 5.1EE.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide LV Rust-Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph only if applicable. If retaining, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Alkyd over Surface-Tolerant Primer System: MPI INT 5.1T.

Prime Coat: Primer, metal, surface tolerant, MPI #23.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Alkyd over Rust-Inhibitive Primer System: MPI INT 5.1TT.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Pittsburgh Paints' "Speedhide Interior/Exterior WB Alkyd" product line, at 50 g/L or less, complies with VOC-content limits in accordance with LEED v4.1.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior, water based, satin (MPI Gloss Level G4).

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Satin, 6-1410XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Alkyd, interior, water based, semi-gloss (MPI Gloss Level G5).

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Semi-Gloss, 6-1510XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Alkyd, interior, water based, gloss (MPI Gloss Levels G6 and G7), MPI #157.

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Gloss, 6-1610XI Series; applied at 1.4 mils minimum DFT.

Alkyd over Shop-Applied Quick-Drying Shop Primer System: MPI INT 5.1W.

Prime Coat: Primer, quick dry, for shop application, MPI #275.

Pittsburgh Paints; Quick Dry Shop Coat Primer, 4190 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Quick-Dry Enamel System: MPI INT 5.1A.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Alkyd, quick dry, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, quick dry, semigloss (MPI Gloss Level G5), MPI #81.

Pittsburgh Paints: HPC Alkyd Semi-Gloss, 4306 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Urethane Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, quick dry, gloss (MPI Gloss Levels G6 and G7), MPI #96.

Pittsburgh Paints; Fast Dry 35 Interior/Exterior Alkyd Gloss, 95-912 Series; applied at 1.0 mil minimum DFT.

Pittsburgh Paints; HPC Urethane Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

Alkyd, Dry-Fall System: [MPI INT 5.1D] [MPI INT 5.1DD].

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Retain one of two "Prime Coat" subparagraphs below for field-applied prime coat. First corresponds to MPI INT 5.1D; second corresponds to MPI INT 5.1DD.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide LV Rust-Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph only if applicable. If retaining, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Dry fall, alkyd, flat, MPI #55.

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Flat 6-160XI Series; applied at 2.3 mils minimum DFT.

Topcoat: Dry fall, alkyd, eggshell (MPI Gloss Level G3).

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Eggshell 6-151XI Series; applied at 1.6 mils minimum DFT.

Topcoat: Dry fall, alkyd, semi-gloss (MPI Gloss Level G5), MPI #225.

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Low Lustre Semi-Gloss 6-161XI Series; applied at 3.1 mils minimum DFT.

Alkyd Dry-Fall over Quick-Drying Primer System: MPI INT 5.1ZZ.

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Prime Coat: Primer, quick dry, for shop application, MPI #275.

Pittsburgh Paints; Quick Dry Shop Coat Primer, 4190 Series; applied at 2.0 mils minimum DFT.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Dry fall, alkyd, flat, MPI #55.

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Flat 6-160XI Series; applied at 2.3 mils minimum DFT.

Topcoat: Dry fall, alkyd, eggshell (MPI Gloss Level G3).

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Eggshell 6-151XI Series; applied at 1.6 mils minimum DFT.

Topcoat: Dry fall, alkyd, semi-gloss (MPI Gloss Level G5), MPI #225.

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Low Lustre Semi-Gloss 6-161XI Series; applied at 3.1 mils minimum DFT.

Aluminum Paint System: [MPI INT 5.1M] [MPI INT 5.1MM].

Retain one of two "Prime Coat" subparagraphs below for field-applied prime coat. First corresponds to MPI INT 5.1M; second corresponds to MPI INT 5.1MM.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide LV Rust-Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph only if applicable. If retaining, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Galvanized metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate primers.

Galvanized Metal Substrates:

Latex System: MPI INT 5.3J.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level 2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level 3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level 4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level 5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 5.3N.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 5.3M.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 5.3K.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Water-Based Dry-Fall System: MPI INT 5.3H.

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Prime Coat: Dry fall, water based, for galvanized steel, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level G1).

Pittsburgh Paints; Speedhide Super Tech WB Interior Latex Dry Fog, Flat 6-725XI Series; applied at 2.2 mils minimum DFT.

Topcoat: Dry fall, water based, for galvanized steel (MPI Gloss Level G3).

Pittsburgh Paints; Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Eggshell 6-724XI Series; applied at 2.0 mils minimum DFT.

Topcoat: Dry fall, water based, for galvanized steel (MPI Gloss Level G5).

Pittsburgh Paints; Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Semi-Gloss 6-727XI Series; applied at 2.2 mils minimum DFT.

Alkyd System: MPI INT 5.3L.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior, flat (MPI Gloss Level G1), MPI #49.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, Interior, Semi-Gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, Interior, Gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Alkyd Dry-Fall System: MPI INT 5.3P.

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Dry fall, alkyd, flat, MPI #55.

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Flat 6-160XI Series; applied at 2.3 mils minimum DFT.

Topcoat: Dry fall, alkyd, eggshell (MPI Gloss Level G3).

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Eggshell 6-151XI Series; applied at 1.6 mils minimum DFT.

Topcoat: Dry fall, alkyd, semi-gloss (MPI Gloss Level G5), MPI #225.

Pittsburgh Paints; Speedhide Interior Alkyd Dry Fog, Low Lustre Semi-Gloss 6-161XI Series; applied at 3.1 mils minimum DFT.

Aluminum Paint System: MPI INT 5.3Q.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints' "Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series" is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Aluminum (Not Anodized or Otherwise Coated) Substrates:

Latex System: MPI INT 5.4H.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 5.4G.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 5.4F.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Aluminum Paint System: MPI INT 5.4D.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Water-Based Light Industrial Coating System: MPI INT 5.4E.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 5.4J.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Copper Substrates:

Latex System: MPI INT 5.5H.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 5.5G.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 5.5F.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 5.5E.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI INT 5.5D.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Stainless Steel Substrates:

Latex System: MPI INT 5.6H.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 5.6G.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: [MPI INT 5.6A] [MPI INT 5.6F].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 5.6A; second corresponds to MPI INT 5.6F.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints: Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI INT 5.6E.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

INTERIOR PAINTING SCHEDULE, WOOD SUBSTRATES

Glued-Laminated Wood Substrates:

Latex over Latex Primer System: MPI INT 6.1M.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Primer System: MPI INT 6.1A.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53] [(MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 6.1Q.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 6.1N.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Alkyd System: MPI INT 6.1B.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Exposed Wood Framed Substrates:

Latex over Latex Primer System: MPI INT 6.2D.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Primer System: MPI INT 6.2A.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 6.2L.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 6.2B.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Alkyd System: MPI INT 6.2C.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Finish Carpentry Substrates: [Wood trim] [Doors] [Windows] [and] [Wood board paneling].

Latex over Latex Primer System: MPI INT 6.3T.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Primer System: MPI INT 6.3U.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 6.3V.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 6.3A.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 6.3P.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 6.3B.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Water-Based Alkyd System: MPI INT 6.3BB.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

Topcoat: Alkyd, water based, satin (MPI Gloss Level G4).

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Satin, 6-1410XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Alkyd, water based, semi-gloss (MPI Gloss Level G5).

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Semi-Gloss, 6-1510XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Alkyd, water based, gloss (MPI Gloss Levels G6 and G7), MPI #157.

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Gloss, 6-1610XI Series; applied at 1.4 mils minimum DFT.

Architectural Woodwork Substrates: [Wood paneling] [and] [Casework].

Latex over Latex Primer System: MPI INT 6.4R.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Sealer System: MPI INT 6.4A.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 6.4T.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 6.4S.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints's "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series " for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 6.4N.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 6.4B.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Wood Traffic Substrates: [Floors] [and] [stairs].

Latex Porch and Floor Enamel System: MPI INT 6.5G.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Floor paint, latex, matching topcoat.

Pittsburgh Paints' "Floor & Porch (3-510XI and 3-610 Series)" enamels are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less (CARB Floor Coatings).

Topcoat: Floor paint, latex, low gloss (maximum MPI Gloss Level G3).

Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510XI Series; applied at 1.0 mil minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Alkyd Floor Enamel System: MPI INT 6.5A.

Prime Coat: Floor enamel, alkyd, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

Intermediate Coat: Floor enamel, alkyd, matching topcoat.

Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level G6).

Pittsburgh Paints; Floor & Porch Waterborne Alkyd Gloss, 3-610 Series; applied at 1.3 mils minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Wood Shingle and Shake Substrates:

Latex over Latex Primer System: MPI INT 6.6F.

Prime Coat: Primer, latex, for interior wood, MPI #39.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Primer System: MPI INT 6.6A.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 6.6B.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

INTERIOR PAINTING SCHEDULE, GYPSUM-BASED SUBSTRATES

Gypsum Board and Plaster Substrates:

Latex over Latex Sealer System: MPI INT 9.2A.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints' "Speedhide 6-2," "Speedhide 6-4900XI," and "Pure Performance 9-900" primers comply with wet-applied VOC content limits and emission requirements of LEED v4.1.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Primer System (for Plaster Only): MPI INT 9.2K.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 9.2M.

Prime Coat: Primer sealer, interior, institutional low odor/VOC, MPI #149.

Pittsburgh Paints; Speedhide Zero Interior Latex Sealer, 6-4900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance 100% Acrylic Latex Primer, 9-900 Series; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

"High-Performance Architectural Latex System" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

High-Performance Architectural Latex System: MPI INT 9.2B.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI INT 9.2L.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints' "Speedhide 6-2," "Speedhide 6-4900XI," and "Pure Performance 9-900" primers comply with wet-applied VOC content limits and emission requirements of LEED v4.1.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd over Latex Sealer System: MPI INT 9.2C.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints' "Speedhide 6-2," "Speedhide 6-4900XI," and "Pure Performance 9-900" primers comply with wet-applied VOC content limits and emission requirements of LEED v4.1.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Water-Based Alkyd System: MPI INT 9.2CC.

Prime Coat: Alkyd, water-based primer sealer, interior, MPI #50.

Pittsburgh Paints' "Speedhide 6-2," "Speedhide 6-4900XI," and "Pure Performance 9-900" primers comply with wet-applied VOC content limits and emission requirements of LEED v4.1.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

Pittsburgh Paints' "Speedhide Interior/Exterior WB Alkyd" product line, at 50 g/L or less, complies with VOC content limits in accordance with LEED v4.1.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, water based (MPI Gloss Level G4).

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Satin, 6-1410XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Alkyd, water based, semi-gloss (MPI Gloss Level G5).

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Semi-Gloss, 6-1510XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Alkyd, water based, gloss (MPI Gloss Levels G6 and G7), MPI #157.

Pittsburgh Paints; Speedhide Interior/Exterior WB Alkyd Gloss, 6-1610XI Series; applied at 1.4 mils minimum DFT.

INTERIOR PAINTING SCHEDULE, MISCELLANEOUS SUBSTRATES

Fiberglass Substrates:

Latex System: [MPI INT 6.7A] [MPI INT 6.7AA].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.7A; second corresponds to MPI INT 6.7AA.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Pittsburgh Paints' "Speedhide Pro-EV Zero," "Speedhide," "Speedhide Zero," and "Pure Performance" product lines comply with VOC content and emission requirements in accordance with LEED v4.1.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior *Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 6.7J.

Retain one of two "Prime Coat" subparagraphs below.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

High-Performance Architectural Latex System: [MPI INT 6.7H] [MPI INT 6.7HH].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.7H; second corresponds to MPI INT 6.7HH.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: [MPI INT 6.7C] [MPI INT 6.7CC].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.7C; second corresponds to MPI INT 6.7CC.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1, Pre-Catalyzed Acrylic Eggshell Epoxy, 16-310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: [MPI INT 6.7B] [MPI INT 6.7BB]:

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.7B; second corresponds to MPI INT 6.7BB.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Plastic Trim Fabrication Substrates:

Latex System: [MPI INT 6.8E] [MPI INT 6.8EE]:

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.8E; second corresponds to MPI INT 6.8EE.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 6.8F.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

High-Performance Architectural Latex System: [MPI INT 6.8A] [MPI INT 6.8AA].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.8A; second corresponds to MPI INT 6.8AA.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Water-Based Light Industrial Coating System: [MPI INT 6.8C] [MPI INT 6.8CC].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI INT 6.8C; second corresponds to MPI INT 6.8CC.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, interior, water based, (MPI Gloss Level G3), MPI #151.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, semi-gloss (MPI Gloss Level G5), MPI #153.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level G6), MPI #154.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 6.8B.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints' "Seal Grip 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip 17-921XI Series" for emissions compliance with LEED v4.1.

Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Spray-Textured Ceiling Substrates:

Latex, Flat System: MPI INT 9.1A, spray applied.

For a Premium Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Budget Grade system.

Prime Coat: Latex, interior, flat, matching topcoat.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Latex System: MPI INT 9.1E, spray applied.

Prime Coat: Latex, interior, matching topcoat.

For Budget and Premium Grade systems, "MPI Manual" requires intermediate coat.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Latex over Alkyd Sealer System: MPI INT 9.1B.

For a Premium Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Budget Grade system.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd over Alkyd Sealer System: MPI INT 9.1D.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Acoustic Panels and Tiles:

Latex, Flat System: MPI INT 9.3A.

Prime Coat: Latex, interior, matching topcoat.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Latex over Alkyd Sealer System: MPI INT 9.3B.

Prime Coat: Primer sealer, alkyd, interior, MPI #45.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 9.3D.

Prime Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

High-Performance Architectural Latex System: MPI INT 9.3E.

Prime Coat: Latex, interior, high-performance architectural, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, high-performance architectural, (MPI Gloss Level G1), MPI #142.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G2), MPI #138.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G3), MPI #139.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural (MPI Gloss Level G4), MPI #140.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #141.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Canvas and Cotton Insulation-Covering Substrates: Including [pipe and duct coverings] <Insert description>.

Latex System: MPI INT 10.1A.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints; Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints; Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Institutional Low-Odor/VOC Latex System: MPI INT 10.1D.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level G1), MPI #143.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G2), MPI #144.

Pittsburgh Paints; Speedhide Max Interior Latex Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G3), MPI #145.

Pittsburgh Paints; Speedhide Max Interior Latex Satin, 6-9410 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level G4), MPI #146.

Pittsburgh Paints; Speedhide Max Interior Latex Lo Lustre, 6-9610 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, institutional low odor/VOC, semi-gloss (MPI Gloss Level G5), MPI #147.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Prominence Interior 100 percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT.

Alkyd System: MPI INT 10.1B.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI INT 10.1C.

Prime Coat: Primer sealer, latex, interior, MPI #50.

Pittsburgh Paints: Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mil minimum DFT.

Pittsburgh Paints: Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Bituminous-Coated Substrates:

Latex System: MPI INT 10.2A.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, interior, flat (MPI Gloss Level G1), MPI #53.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G2), MPI #44.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G3), MPI #52.

Pittsburgh Paints; Speedhide Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series; applied at 1.3 mils minimum DFT.

Topcoat: Latex, interior (MPI Gloss Level G4), MPI #43.

Pittsburgh Paints; Speedhide Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.4 mils minimum DFT.

Topcoat: Latex, interior, semi-gloss (MPI Gloss Level G5), MPI #54.

Pittsburgh Paints; Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT.

Topcoat: Latex, interior, gloss (MPI Gloss Level G6, except minimum gloss of 65 units at 60 degrees), MPI #114.

Pittsburgh Paints; Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI INT 10.2B.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, interior (MPI Gloss Level G3).

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Alkyd, interior, semi-gloss (MPI Gloss Level G5), MPI #47.

Pittsburgh Paints; Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, interior, gloss (MPI Gloss Levels G6 and G7), MPI #48.

Pittsburgh Paints; Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI INT 10.2C.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT.

Pittsburgh Paints; 7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

END OF SECTION 099124